## Slide 1
Metal Forming

## Slide 2
Fundamentals of Metal Forming
Bulk deformation
Sheet metalworking
Outline

## Slide 3: Plastic Deformation
A
Max Load
Elastic region
Plastic region
Notes:   Prior to True stress (TS), the stress in the specimen is uniformly distributed.
  After TS, necking occurs with localization of the deformation to the necking area, which will rapidly go to failure.

## Slide 4
Better accuracy
Better Surface finishing
Strain hardening increase strength
Costs
Temperature in metal forming

## Slide 5: Preferred Orientation
Plastic deformation of idealized (equiaxed) grains in a specimen subjected to compression (such as occurs in the rolling or forging of metals): (a) before deformation; and (b) after deformation. Note the alignment of grain boundaries along a horizontal direction; this effect is known as preferred orientation.

## Slide 6: Recrystallization

## Slide 7
Metal forming performed at room temp or slightly above (below their recrystallisation temperature
Advantage
Better accuracy
Better Surface finishing
Strain hardening increase strength
Costs
Disadvantage
Higher forces are required
Care the surface
Ductility is limited.
Cold Working

## Slide 8
Cracks
Figure (a) and (b) The effect of elongated inclusions (stringers) on cracking, as a function of the direction of bending with respect to the original rolling direction of the sheet. (c) Cracks on the outer surface of an aluminum strip bent to an angle of 90o. Note the narrowing of the tope surface due to the Poisson effect.
(a)
(b)
(c)

## Slide 9
T above Recrystallization Temp.
0. 5Tm < T < 0.75Tm)
Advantage
  The shape can be significantly altered
  Lower forces are required
  Fracture can be reduced
  Strength properties are generally isotropic
  No strengthing of the part occurs from work hardening
  Disadvantage
  Lower dimensional accuracy, higher energy, poorer surface finish
  Shorter tool life
Hot working

## Slide 10
0.3Tm < T < 0.5Tm
Warm Working
Advantage
  Lower forces are required
  More intricate work geometries possible
  The need for annealing may be reduced

## Slide 11: Isothermal
For high speed steel, titanium alloy, good hot hardness
Quick heat transfer
- Raising strength leading to high residual stress
Cracking

## Slide 12: Metal forming process
1. Bulk deformation processes
2. Sheet metal working processes

## Slide 13: Bulk Deforming Processes
• Forging
(wrenches, crankshafts)
• Drawing
(rods, wire, tubing)
often at
elev. T
• Rolling
(I-beams, rails)
• Extrusion
(rods, tubing)

## Slide 14
Extrusion
Metal forced/squeezed out through a hole (die)
Typical use: ductile metals (Cu, Steel, Al, Mg), Plastics, Rubbers
Common products:
Al frames of white-boards, doors, windows, …
[source:www.magnode.com]

## Slide 15
Drawing
Commonly used to make wires from round bars
Similar to extrusion, except: pulling force is applied

## Slide 16: Continuous Drawing

## Slide 17: Sheet Metalworking
• Bending
• Deep drawing
• Shearing

## Slide 18
Forging
[Heated] metal is beaten with a heavy hammer to give it the required shape
Hot forging,
open-die

## Slide 19
Forging
(a)
(b)
Figure 14.1 (a) Schematic illustration of the steps involved in forging a bevel gear with a shaft. Source: Forging Industry Association. (b) Landing-gear components for the C5A and C5B transport aircraft, made by forging. Source: Wyman-Gordon Company.

## Slide 20
Quality of forged parts
Stronger/tougher than cast/machined parts of same material
Surface finish/Dimensional control:
Better than casting (typically)
[source:www.scotforge.com]

## Slide 21: Grain Flow Pattern of Pierced Round Billet
Figure 14.12 A pierced round billet, showing grain flow pattern. Source: Courtesy of Ladish Co., Inc.

## Slide 22: Grain Flow Comparison
Figure 14.3 A part made by three different processes, showing grain flow. (a) casting, (b) machining, (c) forging. Source: Forging Industry Association.

## Slide 23: Upsetting
Figure (a) Solid cylindrical billet upset between two flat dies. (b) Uniform deformation of the billet without friction. (c) Deformation with friction. Note barreling of the billet caused by friction forces at the billet-die interfaces.

## Slide 24: Impression-Die Forging
Figure 14.6 Stages in impression-die forging of a solid round billet. Note the formation of flash, which is excess metal that is subsequently trimmed off (see Fig. 14.8).

## Slide 25: Forging a Connecting Rod
Figure (a) Stages in forging a connecting rod for an internal combustion engine. Note the amount of flash required to ensure proper filling of the die cavities. (b) Fullering, and (c) edging operations to distribute the material when preshaping the blank for forging.

## Slide 26: Trimming Flash from a Forged Part
Figure. Trimming flash from a forged part. Note that the thin material at the center is removed by punching.

## Slide 27: Flashless forging

## Slide 28: Normal

## Slide 29: Flashless Forging

## Slide 30: Comparison of Forging With and Without Flash
Figure 14.9 Comparison of closed-die forging to precision or flashless forging of a cylindrical billet. Source: H. Takemasu, V. Vazquez, B. Painter, and T. Altan.

## Slide 31: Unit Cost in Forging
Figure Typical unit cost (cost per piece) in forging; note how the setup and the tooling costs per piece decrease as the number of pieces forged increases, if all pieces use the same die.

## Slide 32: Relative Unit Costs of a Small Connecting Rod
Figure .
Relative unit costs of a small connecting rod made by various forging and casting processes. Note that, for large quantities, forging is more economical. Sand casting is the more economical process for fewer than about 20,000 pieces.

## Slide 33
Important Applications:
Steel Plants,
Raw stock production (sheets, tubes, Rods, etc.)
Screw manufacture
Rolling

## Slide 34
Rolling Basics
Screw manufacture:

## Slide 35
Rolling
Hot-rolling
Cold-rolling

## Slide 36: Rolling Theory
θ
L=contact length
R=roll radius
p=roll pressure
t0
Roll speed,vt
vt
v0
vt
tt

## Slide 37: Distorted roll
Original shape
Distorted roll
tmin
tmax
Cross section of the sheet

## Slide 38: Rolling force

## Slide 39: Various Configurations
v0
vt
vt
v0
v0
vt
vt
vt
vt
v0
vt
vt
vt
vt
vt
v2
v3
v1
v0
v1
v2
Two high
Three high
Four high
Cluster Mill
Tandem rolling mill

## Slide 40: Cluster Mill

## Slide 41: Shapes Produced by rolling

## Slide 43: Roll-Forging
Figure 14.13 Two examples of the roll-forging operation, also known as cross-rolling. Tapered leaf springs and knives can be made by this process. Source: (a) J. Holub; (b) reprinted with permission of General Motors Corporation.

## Slide 44: Roll piercing
Rolls
Finished
Starting Cylinder
Compressive Force
Tensile
Mandrel
Stresses
Tube

## Slide 45: Friction and lubrication
Friction is undesirable;
  Metal flow in the work is retarded
  The forces to perform are increased
  Rapid wear of tooling
Sticking

## Slide 46: Lubrication
Mineral oils
Graphite
Glass
Graphite in water or mineral oil is a common for hot forging

## Slide 47
Raw material: sheets of metal, rectangular, large
Raw material Processing: Rolling (anisotropic properties)
Processes:
Shearing
Punching
Bending
Deep drawing
Sheet Metal Processes

## Slide 48
Bending
Body of Olympus E-300 camera
component with multiple bending operations
[image source: dpreview.com]
component with punching,
bending, drawing operations

## Slide 49
Shearing
A large scissors action, cutting the sheet along a straight line
Main use: to cut large sheet into smaller sizes for making parts.

## Slide 50
Punching
Cutting tool is a round/rectangular punch,
that goes through a hole, or die of same shape

## Slide 51
Punching
Main uses: cutting holes in sheets; cutting sheet to required shape
typical punched part
nesting of parts
Exercise: how to determine optimal nesting?

## Slide 52
Strip (Scrap)
Blank (Part)
Slug (Scrap)
Part
Piecing
Blanking

## Slide 54
Shearing Operation
Front View
Side View
Die
Punch

## Slide 55
C = at
C = clearance,
a = allowance
t = Thickness (plate)

## Slide 56
How to handle springback:
(a) Compensation: the metal is bent by a larger angle
(b) Coining the bend:
at end of bend cycle, tool exerts large force, dwells
coining: press down hard, wait, release
Bending: springback

## Slide 57
Deep Drawing
Tooling: similar to punching operation,
Mechanics: similar to bending operation
Common applications: cooking pots, containers, …

## Slide 58
Punch Die

## Slide 59
Progressive Die
https://youtu.be/NuFpzJLMnFs?t=88

## Slide 60
Progressive Die Stamping
Fabricating complex parts in earlier days was an inefficient and costly affair. Either a manufacturer could repeatedly change the tool in a single press or use multiple presses each performing single action to produce one part. This resulted in long load times and a high labor cost.
With progressive die stamping, a manufacturer can eliminate all these hassles and produce better quality parts faster and in a cost-effective manner.

## Slide 61
Progressive Die
https://youtu.be/10vNgC4LpkQ?t=113